## Slide 1: Atomic Structure of Grain Boundaries in Graphene
Otho Ulrich1,2, Joseph Gonzalez1, Kien Nguyen Cong1, Dr. Ivan Oleynik1
1 Materials Simulations Laboratory, Dept. of Physics, University of South Florida
2 Dept. of Physics, Western Michigan University
Project supported by the NSF REU grant # DMR-1263066: REU Site in Applied Physics at USF and the Materials Simulation Laboratory, University of South Florida

## Slide 2: Outline
Background & Motivation
Research Objectives
Computational Details
Analyses and Results
Future Studies

## Slide 3: Graphene: Pristine vs. Polycrystalline
One of the strongest materials measured [1]
100 times fracture strength of steel [3]
Multiple grains with relative orientations
Defects present at grain boundaries
Expected degradation of mechanical properties
Lee et al. Science 340 (2013), 3. Kusmartsev et al. arXiv:1406.0809v1 (2014)

## Slide 4: Exfoliation vs. Chemical Vapor Deposition
Exfoliated samples
  Pristine
  Barely exceed ~1mm in length [4]
CVD samples
  Multiple grains and defects (polycrystalline)
  Scale to large samples
2. Rasool et al. Nature Communications (2013), 4. Geim et al. Physics Today 60 (2007)
Polycrystalline graphene. Scale bar .8nm.
[2]
Pristine graphene. Scale bar .8nm.
[2]

## Slide 5: Grain Defects
[5]
[5]
Single vacancy defect.
Double vacancy defect.
5. Banhart et al. ACS Nano 5 (2011)
Structural defects are expected to affect mechanical properties.

## Slide 6: Experimental Methods
“Small grain” polycrystalline graphene.
“Large grain” bicrystalline graphene.
AFM diamond-tip nanoindentation.
Force-displacement curve attained during nanoindentation.
Lee et al . Science 340 (2013), 2. Rasool et al. Nature Communications (2013)
[1]
[1]
[1]
[2]
Identification, nanoindentation, and measurement.

## Slide 7: Experimental Results
[1]
Lee et al . Science 340 (2013), 2. Rasool et al. Nature Communications (2013)
Fracture load and elastic stiffness are not significantly degraded, but fracture load may be a function of angle.
Red – AC
Blue – ZZ
Purple - AC/ZZ
[1]
[2]

## Slide 8: Research Objectives
Predict the formation energy of graphene bicrystals as a function of misorientation angle
Predict fracture strength and Young’s modulus as a function of misorientation angle for graphene bicrystals
Determine trends between formation energies and their effect on mechanical properties

## Slide 9: Computational Details
Environment
  LAMMPS: open-source molecular dynamics suite
  SEDREBO: defines carbon-carbon interaction potential
    Analytical pairwise attractive and repulsive functions
    Cutoff distance beyond the spinodal bond length
    Screening function to preserve only nearest neighbor interactions are taken into account
  Conjugate gradient method minimizes system energy
Graphene Bicrystal Generation
Formation of Unit Cell

## Slide 10: Conjugate Gradient Method
  Atoms are translated from higher to lower potential until they reach a minimum
  SEDREBO defines the potential energy gradient V.

## Slide 11: Graphene Bicrystal Generation
Two grains with misorientation angle θ are procedurally generated
θ=27.8˚
θ=13.9˚

## Slide 12: Formation of Unit Cell
Periodic boundary conditions are applied to the cell
System energy is minimized using conjugate gradient method (SEDREBO defines gradient)
θ=27.8˚
θ=13.9˚

## Slide 13: Analysis of Individual Bicrystals
Formation energy and atomic coordination are used to automatically discard non-physical structures
Energy distribution is used to define defective region
Atomic Energy Distribution
θ=27.8˚
Atomic Energy Distribution
θ=13.9˚
Energy (eV)
Energy (eV)
Displacement in x (Å)
Displacement in x (Å)

## Slide 14: Results
Formation Energy (normalized) Distribution
ΔE/Ly (eV/Å)
Misorientation Angle (deg.)
Conclusion: Formation energy depends on a property other than misorientation angle.

## Slide 15: Future Studies
Subject each unit cell to hydrostatic biaxial strain
From stress-strain curves, generate fracture strength and Young’s modulus distributions as functions of misorientation angle
Determine trends between formation energies of certain grain boundaries and their effect on mechanical properties

## Slide 16: Thank You
National Science Foundation
University of South Florida
Department of Physics
Materials Simulation Laboratory and colleagues
Applied Physics REU program and its coordinators
Fellow REU participants

## Slide 17: Questions

## Slide 18: References
Lee, G., Cooper, R., An, S.J., Lee, S., van der Zande, A., Petrone, N., Hammerberg, A., Lee, C., Crawford, B., Oliver, W., Kysar, J., Hone, J. High-Strength Chemical-Vapor-Deposited Graphene and Grain Boundaries. Science 340, 1073 (2013)
Rasool, H., Ophus, C., Klug, W., Zettl, A., Gimzewski, J. Measurement of the Intrinsic Strength of Crystalline and Polycrystalline Graphene. Nature Communications 10.1038/ncomms3811 (2013)
Kusmartsev, F.V., Wu, W.M., Pierpoint, M.P., Yung, K.C. Application of Graphene within Optoelectronic Devices and Transistors. arXiv:1406.0809v1 [cond-mat.mtrl-sci] (2014)
Geim, A. K., MacDonald, A. H. Graphene: Exploring carbon flatland. Physics Today 60 (8): 35–41 (2007)
Banhart, F., Kotakoski, J., Krasheninnikov, A.V. Structural Defects in Graphene. ACS Nano 5 (1): 26–41 (2011)

## Slide 19: Supplemental Information

## Slide 20: Molecular Dynamics
(1) t=0
(2) t=0, calculate force
(3) t=1, after movement
V
MSL uses molecular dynamics to predict mechanical properties of graphene.
Potential function V is defined by SEDREBO.

## Slide 21: Testing Mechanical Properties
Uniaxial Load
Biaxial Load
Nanoindentation
For each experiment, fracture strength will be determined and indexed by misorientation angle or defect type and distribution.

## Slide 22
[2]
εyy
2. Rasool et al Nature Communications (2013)
Mapping Graphene
Pristine graphene bond lengths.
30o grain boundary bond lengths.
Strain components for 30o grain boundary. -5% (blue) to +5% (red).
εxx
εxy
[2]

## Slide 23: Preliminary Results: Computational Pull-Out Experiment
SEDREBO pull-out animation.
REBO pull-out animation.